SECTION 32 31 13

ARTISTIC LASER CUT ACRYLIC ALUMINUM SCREEN AND GATES

The specifier will need to edit this product specification for a specific project to reflect the options and applications being used.  This guide section has been written to show items to be determined reflected in italic red.  PalmSHIELD does not warrant that these specifications are complete and applicable to all applications.  It is the specifier’s responsibility to assure that use of PalmSHIELD is an appropriate fit for the site and conditions.

PART 1 – GENERAL

  - DESCRIPTION

- This section describes the following screen system:

Fixed laser cut modular fencing panels fabricated with laser cut aluminum sheet and transparent acrylic sheet  including extruded aluminum screen posts and aluminum gates. Laser cut aluminum security screen and gates shall be furnished and installed as shown on the plans and specified herein, overall height of vertical laser cut panel framework shall be (state height here) tall.

  - REQUIREMENTS

- Furnish materials, labor, expertise and equipment necessary to complete all work specified in this section and as shown on the drawings.

- Structural Performance:  Provide product and installation capable of withstanding the effects of gravity loads and the following loads and stresses within limits and under conditions indicated.

    - Uniform pressure of 30 lbf/sq. ft. acting inward or outward.

    - Thermal Movements resulting from a temperature change (range) of 120 degrees Fahrenheit ambient and 180 degrees Fahrenheit material surfaces.

  - SUBMITTALS

- Shop drawings and manufacturer's literature:  Provide specifications and construction detail drawings to substantiate quality of materials and provide details of fabrication and installation.

- Submittals shall be in accordance with standard construction practices to include complete detailed layout of all panels, posts, gates.  Submittals shall include plan layout, elevations and section views of panels, posts and gates.

- Certificate:  manufacturer's certification that materials meet specification requirements.

  - REFERENCES

- ASTM B 209 – Standard Specification for Aluminum and Aluminum-Alloy Sheet 				and Plate.

- ASTM B 221 – Standard Specification for Aluminum and Aluminum-Ally 					Extruded Bars, Rods, Wire, Profiles and Tubes.

- ASTM D3363 – Standard Test Method for Film Hardness by Pencil Test.

- ASTM D2794 – Standard Test Method for Resistance of Organic Coatings to the 				Effects of Rapid Deformation.

- ASTM B117 – Standard Practice for Operating Salt Spray Apparatus.

- ASTM D822 – Standard Practice for Filtered Open-Flame Carbon-Arc Exposures of 			Paint and Related Coatings.

- AWS D1.2 Structural Welding Code – Aluminum.

- ASTM D 638 Standard test methods for testing tensile strength of plastics.

  - QUALITY ASSURANCE

- Installation of screen and materials shall conform to the requirements of the screen manufacturer.

- The screen shall be warranted from any defects in materials and workmanship for a period as specified in the relevant section of the contract documents.

PART 2 – PRODUCTS

  - MATERIALS

- Laser cut security fence:

  - Approved Laser cut Screen System, Manufacturer:

    - “Palm Shield” or approved equal.

- Material Descriptions:

  - ACRYLITE FF  .118 (3 mm) sheet has a  tensile strength of 10,000 psi (69 Mpa) at room temperature (ASTM D 638).

  - Laser cut metal sheet thicknesses shall be (.032”,.040", .050",.063", .080" .125", .250)

  - Pattern is (state pattern type here.)

  - Extruded Aluminum: ASTM B 221, Alloy 6063 – Temper T-6.

  - Sheet Aluminum: ASTM B211, Alloy 6063 – Temper T6.

  - Powder Coating Material Hardness: ASTM 3363 2H.

  - Panel Description:

    - Panel Height: (state height here)

    - Acrylic backed laser cut  Panel Width: Not to exceed 6’.

    - Acrylic laser cut  fencing system consisting of laser cut sheet with backing sheet. Laser cut, modular screen panels fabricated with extruded aluminum framing and supported by extruded aluminum screen posts.

    - Vertical Framework: 3 inch x 3 inch x ¼ inch aluminum angle. Framework supporting the laser cut sheet shall be solid welded and mitered.

    - Horizontal Top Cap: 3 inch x 3 inch x ¼ inch aluminum top 	cap.

    - Horizontal Bottom Cap: 3 inch x 3 inch x ¼ inch angle bottom cap.

    - Cross Bar: 2 inch x 1/8 inch aluminum flat bar.

  - Screen Posts:

    - Panel posts shall be 4 inch square by ¼ inch minimum extruded tubular aluminum sections with solid aluminum caps. Length as specified on the contract drawings.

    - On center post spacing shall be as specified by manufacturer.

    - All screen posts to be plated with 10” x 10” x ¾” aluminum plates with four ¾” hole for anchors.

  - Fittings and accessories:  All fittings and accessories shall be stainless steel and sized as specified by the screen manufacturer. Screen panels to be attached to posts with ¼” x 1” stainless steel screws.  Panels and posts are predrilled to support level installation.

  - Anchor Bolts: Anchor bolts shall be (state means of anchoring posts to adjoining surface. Please see our installation instructions for recommendations.) and adequate to support loads based on screen ing height, exposures and loading.

  - Gates:  Swing to exterior of enclosure, size as shown on contract drawings.

    - Laser cut panel style and appearance shall be identical to screen panels.

    - Gate hinges to be Gorilla barrel hinge with ¾” rod, ball bearing, and grease zert.  Hinge plate to be ½” thick plates offset to create a 5/8” gap.  Standard hardware as required by the gate manufacturer for complete functional operation.  Hinges to be bolted to gate frame and field welded to steel gate posts.

    - Gate latch to be internal lock with exterior grab handles.  Lock may be keyed and rekeyed.  Lock is accessible from both sides of gate.

    - Welded frame, size as shown on the contract drawings, extruded aluminum tubing with aluminum laser cut panels to match fencing material.

    - Drop rods to be 1” schedule 40 pipe and through bolted to gate frame.

    - Hardware: Size and type as determined by the manufacturer. Provide three hinges per leaf.

      - Provide 1 inch diameter center cane bolt assembly and strike, each door.

      - Provide padlockable slide bolt assembly.

    - Gate shall have welded frame fabricated from extruded aluminum tubing with aluminum fixed laser cut panels to match fencing material.  Frame configurations shall be as indicated on the contract drawings.

    - Gate posts shall be as determined by manufacture.  Gate posts to be specified to support gates.

6.	Factory Finish: Aluminum screen panels, posts and gates shall receive 	polyester powder coating.

a.	Polyester powder coating: Electrostatically applied colored polyester 			powder coating heat cured to chemically bond finish to metal 			substrate.

b.	Color shall be as selected by Owner.

c.	Minimum hardness measured in accordance with ASTM D3363 2H.

d.	Direct impact resistance tested in accordance with ASTM D2794. 			Withstand 160 inch-pounds.

e.	Salt spray resistance tested in accordance with ASTM B117: No 			undercutting, rusting, or blistering after 500 hours in 5 percent salt 			spray at 95° F and 95% relative humidity after 1,000 hours, less than 			3/16 inches undercutting.

f.	Weatherability tested in accordance with ASTM D822: No film 			failure and 88 percent gloss retention after 1 year exposure in South 			Florida with test panels tilted 45°.

PART 3 – EXECUTION

  - INSPECTION

  - Verify that final grading in screen location is completed and without irregularities which will interfere with screen installation.  PalmShield is designed to be installed on a level surface.  Variations in height, slopes, stairs steeping shall be shown on contract drawings and on submittal drawings.

  - Field verify all screen dimensions and layout prior to commencing installation.

  - Do not commence work until unsatisfactory conditions have been corrected.

3.2	INSTALLATION

- Install screen in accordance with manufacturer’s installation instructions.

- Install screen plumb and level. Posts are plated and mounted to top of surface.

- Do not install bent, bowed or otherwise damaged panels. Remove damaged components from site and replace.

- Secure screen panels with stainless with ¼” x 1” stainless steel screws to screen posts. All posts and panels will be predrilled to support level installation.

- Gates

  - Install gates and adjust hardware for smooth operation